SECTION  084413  (08920)

2500 ALUMINUM CURTAIN WALL

This suggested guide specification has been developed using the current edition of the Construction Specifications Institute (CSI) “Manual of Practice”, including the recommendations for the CSI 3 Part Section Format and the CSI Page Format.  Additionally, the development concept and organizational arrangement of the American Institute of Architects (AIA) MASTERSPEC Program have been recognized in the preparation of this guide specification.  The preparation of the guide specification assumes the use of standard contract documents and forms, including the “Conditions of the Contract”, published by the AIA.

PART 1 – GENERAL

1.01	Summary

A.	Section includes:	CAPITOL 2500 WALL Aluminum Curtain Wall Systems

1.	Types of CAPITOL Aluminum Curtain Wall Include:

a.	2500 Wall System - 2 1/2” x 5 1/2”, outside glazed

b.	2500 Wall System - 2 1/2” x 6 1/2”, outside glazed

c.	2500 Wall System - 2 1/2” x 7 1/2”, outside glazed

d.	2500 Wall System - 2 1/2” x 8 3/4”, outside glazed

ED NOTE:  Below related sections are specified elsewhere, however, CAPITOL

recommends single source responsibility for all of these sections as indicated in

2.07 source quality control.

B.	Related sections:

1.	Section 085113 - Aluminum Windows

2.	Section 087100 - Hardware

3.	Section 084413 - Aluminum Curtain Wall System

- Section 088000 – Glazing

- Section 079200 – Sealants

6.	Section 107113 – Exterior Sun Control Devices

1.02	References (Industry Standards)

ED NOTE:  Refer to index for any and all applicable standards.

1.03	System Description

A.	Curtain Wall System Performance Requirements:

1.	Air Infiltration:	The test specimen shall be tested in accordance with ASTM E 283.  			Air infiltration rate shall not exceed 0.06 CFM/ft2 at a static air pressure differential of 				6.24 psf.

2.	Water Resistance:  The test specimen shall be tested in accordance with ASTM E 					331.  There shall be no leakage at an air pressure differential of 12 psf as defined in

AAMA 501.

3.	Uniform Load:	A static air design load of 40 psf shall be applied in the positive 				and negative direction in accordance with ASTM E 330.  There shall be no deflection in 				excess of L/175 of the span of any framing member at design load.  At structural test load

equal to 1.5 times the specified design load, no glass breakage or permanent set in the 				framing members in excess of 0.2% of their clear spans shall occur.

1.03	System Description (continued)

NOTE:  Coordinate wind loads with applicable building code, or appropriate wind loads may be 		determined by using ANSI A58.1-1982, “Minimum Design Loads for Buildings and Other 			Structures”.  An allowable deflection less than 1/175 of clear span is industry standard.  Smaller 		deflections will often require use of heavier cross sections or internal reinforcements.

4.	Thermal Performance tested to AAMA 1503.98, the thermal transmittance (U-factor) not 				more than 0.52 (low-e).

5.	Thermal Performance tested to NFRC102-2004, the thermal transmittance (U-factor) not 				more than 0.49 (low-e).

6.	Condensation Resistance (CRF):  When tested to AAMA 1503.98 the condensation factor 			not less than 62 (frame) and 62 (glass-low-e).

7.	Sound Transmission (STC) tested to ASTM E 90, the sound transmittance not less than 				32 when glazed with 1" insulated glass or not less than 48 when glazed with 1" insulated 				glass with blind sash.

8.	Requirements shown by details are intended to establish basic dimension of unit, sight 				lines and profiles of members.

9.	Do not assume glass, sealants and interior finishes contribute to framing member 					strength, stiffness or lateral stability.

10.	Assemblies shall be free from rattles, wind whistles and noise due to thermal and 					structural movement and wind pressure.

11.	Attachment considerations are to take into account site peculiarities and expansion and 				contraction movements so there is no possibility of loosening, weakening or fracturing 				connection between units and building structure or between units themselves.

12.	Allow for expansion and contraction without detriment to appearance or performance.

13.	System shall drain to the exterior of system any water entering system.

1.04	Submittals

A.	General:	Submit in accordance with Section 013000.

B.	Product Data:

1.	Submit manufacturer’s descriptive literature for each manufactured product.

2.	Include information for factory finishes, accessories and other required components.

C.	Shop Drawings:

1.	Submit drawings indicating elevations, detailed design, dimensions, member profiles, 				joint locations, arrangement of units and member connections.

2.	Show following items:

a.	Details of special shapes.

b.	Reinforcing.

c.	Anchorage system.

d.	Interfacing with building construction.

e.	Provisions for expansion and contraction.

f.	Thermal breaks

3.	Indicate typical glazing details, (locations of various types and thickness of glass), and 				internal sealant requirements as recommended by sealant manufacturer.

4.	Clearly indicate locations of fasteners and joints for Architect’s acceptance.

D.	Test Reports:	Submit certified copies of previous test reports by independent laboratory 				substantiating performance of system.  Include other supportive data as necessary.

1.04	Submittals (continued)

E.	Certificates:

1.	Submit manufacturer’s certification stating that installed system is in compliance with 				specified requirements.

F.	Qualification Data:

1.	Submit installer qualifications verifying years of experience.

2.	Include list of projects having similar scope of work identified by name, location, date, 				reference name and phone number.

G.	Manufacturer’s Instructions:

1.	Submit manufacturer’s printed installation instructions.

H.	Warranty:

1.	Submit specified warranties.

1.05 	Warranty

A.	Project Warranty:	Refer to “Conditions of the Contract” for project warranty provisions.

B.	Manufacturer’s Product Warranty:	Submit, for Owner’s acceptance, manufacturer’s warranty 			for curtain wall system as follows:

1.	Warranty Period:	One (1) year from last date of shipment by Capitol Aluminum and

Glass Corporation.

1.06	Quality Assurance

A.	Qualifications:

1.	Installer Qualifications:  Installer experienced to perform work of this section who has 				specialized in the installation of work similar to that required for this project and who is 				acceptable to product manufacturer.

2.	Manufacturer Qualifications:  Manufacturer capable of providing field service 					representation during construction, approving acceptable installer and approving 					application method.

3.	Per-Installation Meeting:  Conduct pre-installation meeting to verify project 					requirements, substrate conditions, manufacturer’s installation instructions and 					manufacturer’s warranty requirements.

1.07	Delivery, Storage and Handling

A.	Ordering:  Comply with manufacturer’s ordering instructions and lead time requirements to 			avoid construction delays.

B.	Packing, shipping, handling and unloading:  Deliver materials in manufacturer’s original, 				unopened, undamaged containers with identification labels intact.

C.	Storage and protection:  Store materials protected from exposure to harmful weather conditions.  			Handle material and components to avoid damage.

PART 2 – PRODUCTS

2.01	Manufacturers (Acceptable Manufacturers/Products)

A.	Acceptable manufacturers:

1.	Capitol Aluminum & Glass Corporation, 1276 W. Main Street, Bellevue, OH  44811

(419) 483-7050 - (419) 483-7830 fax

Proprietary Product(s)/System(s):	CAPITOL 2500 WALL Aluminum Curtain Wall

Finish/Color (See Section 2.06 Finishes)

NOTE:	  Consult with CAPITOL for recommendations on alternate manufactures and products 			meeting the design criteria and project requirements.  CAPITOL recommends other 				manufacturers requesting approval to bid their product as an equal must submit their request in 			writing ten (10) days prior to close of bidding.

2.02	Materials

A.	Aluminum (Curtain Wall and Components):

1.	Material Standard:	Extruded Aluminum, ASTM B 221, 6063-T5 alloy and temper.

2.	Member Wall Thickness:	Each framing member shall have a wall thickness sufficient 			to meet the specified structural requirements.

3.	Tolerances:	Reference to tolerances for wall thickness and other cross-sectional 				dimensions of curtain wall members are nominal and in compliance with AA Aluminum 				Standards and Data.

2.03	Accessories

A.	Fasteners:

1.	Aluminum, non-magnetic stainless steel or other materials warranted by manufacturer to 				be non-corrosive and compatible with components being fastened.

2.	For exposed locations, provide countersunk Phillips head screws with finish matching 				items fastened.

3.	For concealed locations, provide manufacturer’s standard fasteners.

B.	Glazing Gaskets:

1.	Compression type design, replaceable, molded or extruded neoprene, or ethylene 					propylene diene monomer (EPDM).

2.	Comply with ASTM C509 or C864.

3.	Profile and hardness as necessary to maintain uniform pressure for watertight seal.

4.	Provide in manufacturer’s standard black color.

C.	Expansion Anchor Devices:  Lead-shield or toothed-steel, drilled-in, expansion bolt anchors.

2.04	Related Materials

A.	Glass and Glazing Accessories:

1.	Refer to Section 088000.

B.	Sealants

1.	Refer to Section 079200.

2.05	System Fabrication

A.	Take accurate field measurements to verify required dimensions prior to fabrication.

B.	Provide rigid, thermal break isolators to prevent exterior and interior aluminum framing 				members from being in contact with each other.

C.	Fabricate components in accordance with approved shop drawings.  Remove burrs and smooth 			edges.  Shop fabricate to greatest extent practicable to minimize field cutting, splicing and 			assembly.  Disassemble only to extent necessary for shipping and handling limitations.

D.	Fabricate components true to detail and free from defects impairing appearance, strength or 			durability.  (Fabricate custom extrusions indicated and as necessary for complete installation.)

E.	Provide structural reinforcing within framing members where required to maintain rigidity and 			accommodate design loads.

F.	Provide holes or slots, deflector plates, water deflectors and sealants to accommodate internal 			weep and drainage to the exterior of curtain wall system.

G.	Allow for adequate clearance around perimeter of system to enable proper installation and for 			thermal movement within system.

H.	Separate dissimilar metals with protective coating to prevent contact and corrosion.

I.	Aluminum integral blinds (Optional)

1.	All curtain wall fixlites shall be furnished with an integral blind.  Owner to select blind color from manufacturers standard.

2.	All blinds to include 5/8” slats with mounting brackets and control knob hardware.  All tilting of blinds shall be performed without accessing the blinds.

3.	The system shall be a hinged, non-lift off type blind sash comprised of extruded aluminum and shall have a nominal wall thickness of .060" and 1/4" glass.  This system shall have a T-slot foam compression seal installed in a specifically designed groove in the extrusion, creating an air-tight seal to keep dust and other debris out. Screw applied lift off dust shield is not acceptable.

4.	The blind operator mechanism shall hold and tilt slats and be mechanically actuated using a positive gear drive system. Magnetic or string type actuators are not acceptable.

a.	Provide manufacturer's standard straight knob blind operator.

b.	Optional flush plate with removable hex key and pole ring

operators available upon request.

2.06 	Finishes

A.	Clear Anodized 30-Minute Velo Class II		AA-M12-C22-A31

Clear Anodized 60-Minute Velo Class I		AA-M12-C22-A41

Dark Bronze Anodized 2-step Class I			AA-M12-C22-A44

Champagne Anodized 2-step Class I			AA-M12-C22-A44

FloroponR (70% PVDF)**				AAMA 2605

DuranarR, DuranarR XL (70%PVDF)**		AAMA 2605

AcroflurTM (50% PVDF)**				AAMA 2604

AcrynarRFX (50% PVDF)**				AAMA 2604

PolylureR 1500**					AAMA 2603

DuracronR** 						AAMA 2603

**manufacturer’s standard colors

2.07	Source Quality Control

A.	Source Quality:	Provide aluminum curtain walls specified herein from a single source.

1.	Building Enclosure System:	When aluminum curtain wall is part of a building enclosure 			system, including entrances, entrance hardware, windows, storefront framing and related 				products, provide building enclosure system products from a single source manufacturer.

PART 3 – EXECUTION

3.01	Examination

A.	Site Verification of Conditions:	Verify substrate conditions (which have been previously 			installed under other sections) are acceptable for product installation in accordance with 				manufacturer’s instructions.  Verify openings are sized to receive curtain wall system and sill 			plate is level in accordance with manufacturer’s acceptable tolerances.

1.	Field Measurements:	Verify actual measurements/openings by field measurements 				before fabrication; show recorded measurements on shop drawings.  Coordinate field 				measurements, fabrication schedule with construction progress to avoid construction 				delays.

3.01	Examination (continued)

a.	Tolerances:

I.	Limit variations from plumb and level:

- 1/8” inch in 20 feet (93 mm in 6 M) vertically and horizontally

- 1/4” inch in 40 feet (6 mm in 12 M) either direction

II.	Limit offsets in theoretical end-to-end and edge-to-edge alignment:

- 1/16” inch (2 mm) where surfaces are flush or less than 1/2” inch (13 						   mm) out of flush and separated by not more than 2” inches (51 mm)

- 1/8” inch (3 mm) for surfaces separated by more than 2” inches (51 mm)

III.	Step in face:	1/16” inch (2 mm) maximum

IV.	Jog in alignment:	1/16” inch (2 mm) maximum

V.	Location:	1/4” inch (6 mm) maximum deviation of any member at 						any location

VI.	Tolerances are not accumulative

3.02	Installation

A.	General:	Install curtain wall systems plumb. Level and true to line, without warp or rack of 			frames with manufacturer’s prescribed tolerances and installation instructions.  Provide support 			and anchor in place.

1.	Dissimilar materials:	Provide separation of aluminum materials from sources of 					corrosion or electrolytic action contact points.

2.	Weather-tight construction:	Install sill members and other members in a bed of sealant 				or with joint filler or gaskets, to provide weather-tight construction.  Coordinate 					installation with wall flashings and other components of construction.

B.	Related Products Installation Requirements:

1.	Sealants (Perimeter):	Refer to Division 7 Joint Treatment (Sealants) Section.

2.	Glass:	Refer to Division 8 Glass and Glazing Section.

a.	Reference:	ANSI Z97.1, CPSC 16 CFR 1201 and GANA Glazing Manual.

3.03	Protection and Cleaning

A.	Protection:	Protect installed Curtain Wall systems finish surfaces from damage during 					construction.  (i.e. grinding, polishing compounds, plaster, lime, acid,

cement, or other harmful contaminants).

B.	Cleaning:	Remove temporary coverings and protection of adjacent work areas.  Repair or 					replace damaged installed products.  Clean installed products in accordance with 					manufacturer’s instructions prior to owner’s acceptance.  Remove construction 					debris from project site and legally dispose of debris.

DISCLAIMER STATEMENT

This guide specification is intended to be used by a qualified construction specifier.  The guide specification is not intended to be verbatim as a project specification without appropriate modifications for the specific use intended.  The guide specification must be used and coordinated with the procedures of each design firm, and the particular requirements of a specific construction project.

END OF SECTION 084413 (08920)